PART 1 - GENERAL

1.01	RELATED DOCUMENTS

Drawings and general provisions of Contract, including General and Supplementary Conditions and Division 1 Specification sections, apply to work of this section.

1.02	WORK INCLUDED

- Brick units.

- Reinforcement, anchors, and accessories.

1.03	WORK INSTALLED BUT FURNISHED UNDER OTHER SECTIONS

- Section 05500 – Miscellaneous Metals:  Loose steel lintels, foundation vents.

- Section 07600 – Flashing and Sheet Metal

- Section 07670 – Thru-Wall Flashing.

1.04	RELATED WORK

- Section 03300 – Cast in Place Concrete.

- Section 04100 – Mortar and Grout.

- Section 06100 - Rough Carpentry.

- Section 07920 - Caulking and Sealant.

1.05	SUBMITTALS

Submit samples of brick to reflect the full range of color, shades and surface texture of brick specified.

1.06	MOCKUP

- As soon as the brick and stone samples have been approved, deliver enough brick to the job site to construct a 6’-0” x 4’-0” sample wall panel, incorporating both metal stud backup and CMU backup.

- Construct the mockup panel using the brick, mortar, reinforcing, weep holes, tooling, and cleaning as specified.

- The approved sample panel shall be standard of workmanship.

- As construction proceeds, the first full panel of brickwork between expansion joints shall become the standard of workmanship for issues, such as head joint alignment, that are not apparent on the smaller mockup panel.

- Mockup panel shall not be removed until masonry work as required by this section has been completed.

1.07	ENVIRONMENTAL CONDITIONS

A.	Follow hot weather and cold weather requirements in the masonry code and specifications, TMS 402 and TMS 602.

  - DELIVERY, STORAGE AND HANDLING OF MATERIALS

Deliver, store, and handle materials to prevent inclusion of foreign materials and damage by water or weather.  Store packaged materials in their original packages.  Damaged or deteriorated materials shall be removed from the premises.

# PART 2 - PRODUCTS

2.01	ACCEPTABLE BRICK MANUFACTURERS

- Products specified are manufactured by Acme Brick Company and are listed as a standard of quality.  Brick shall match __________.

- Substitutions:  Under provisions of Section 01600.

2.02	BRICK UNITS

- Standard Face Brick:  Shall be Brick shall be FBS or HBS and shall be as follows: (Add or removes sizes to fit project requirements.)

  - Modular in size, 2 1/4 x 3 5/8 x 7 5/8 inches, and conform to the requirements of ASTM C 216 or C 652, Grade SW.

  - Kingsize 2 5/8 x 2 5/8 x 9 5/8 inches and conform to the requirements of ASTM C 216 or C 652, Grade SW.  Field cut closers as required for half-bond pattern.

  - Utility 3 5/8 x 3 5/8 x 11 5/8 inches and conform to the requirements of ASTM C 216 or C 652, Grade SW.  Field cut closers as required for half-bond pattern.

  - Utility Closer 3 5/8 x 3 5/8 x 7 5/8 inches and conform to the requirements of ASTM C 216 or C 652, Grade SW.

  - Norman 3 5/8 x 2 1/4 x 11 5/8 inches and conform to the requirements of ASTM C 216 or C 652, Grade SW.  Field cut closers as required for half-bond pattern.

  - Estate 3 5/8 x 3 5/8 x 15 5/8 inches and conform to the requirements of ASTM C 216 or C 652, Grade SW.  Field cut closers as required for half-bond pattern

  - Other sizes as specified and subject to availability

- Special shape face bricks shall be as detailed and at locations as indicated on the drawings.

- Furnish special uncored face brick in locations where cores would be exposed in finish work.

2.03	ANCHORS AND TIES

- Acceptable Manufacturers:

- Products of Hohmann and Barnard and Heckman Bldg. Products, conforming to specification requirements are acceptable.

- Substitutions:  Under provisions of the General Provisions.

- Anchors:

- Slotted anchors of type DW10 shall be used with steel stud or wood stud backup walls, UNO.

- Dur-O-Eye or equal anchors welded to joint reinforcing shall be used with masonry backup walls.  Missing or damage anchors shall be replaced as necessary with DW19 anchors fastened to wall with corrosion resistant Tapcon screws.

- Anchors and ties for stone veneer shall be as recommended by the manufacturer.

- Zinc coating shall comply with ASTM A153-B2.

2.04	ACCESSORIES

- Weep Holes:  Open head joints every third brick at lintels and other locations.

- Compressible Filler:  Premolded, flexible cellular neoprene rubber filler strips complying with ASTM D 1056, Grade RE41E1, capable of compression up to 35% of width and thickness indicated.

- Mortar Net:  Provide continuous Mortar Net along base of air space to catch mortar drippings.  High-density polyethylene, 90% open mesh, dovetail shape.

- As an alternate to Mortar Net, every third brick may be left out at base of air space and cavity cleaned and inspected to be free of mortar droppings.

## PART 3 - EXECUTION

  - LAYING AND SETTING BRICK

- Pre-wet all brick having initial rate of absorption greater than 30 before laying.

- Heat water and sand in cold weather.  Do not lay brick in temperature below freezing unless such heating of materials and protection of work is properly provided for.

- The exterior surfaces of concrete and concrete masonry backup walls shall be damp-proofed before face brick are laid.

- All brickwork shall be laid true to dimensions, plumb, square, and in bond.  All courses shall be level with joints of uniform width and height.

- Vertical joints in facing bond work shall be spaced so as to line up plumb and true, and all joints shall be as uniform as the type of brick will allow.

- Lay facing brick in full mortar bed with shoved head joints.  Completely fill joints with mortar.  Do not deep furrow bed joints.

- Allow space for caulking of joints at frames.

- Bond for facing brick shall be running bond or as shown on drawings.  Match existing bond patterns unless noted otherwise.

- Anchor facing brick to metal studs or masonry backup at 16 inches o.c. vertically and 16 inches o.c. horizontally with adjustable anchors and ties.

- Joint thickness shall be such as to provide coursing pattern to match existing brickwork.  When the joints have become thumbprint hard, all exposed joints shall be tooled with a sled-jointing tool.  The jointer shall be larger than the width of the joints so that a complete contact is made along the edges of the units, compressing and sealing the surface of the joint.  Joints shall be pointed as the tool proceeds.

- Form weep holes in head joints at face brick over shelf angles and lintels and where shown on the drawings. Rake out bed joint mortar to clean flashing surface.  Weep holes shall be filled with preformed mesh type vent at bottom of head joints not more than 24 inches o.c.

- Keep air space clean of mortar at all times.  Where brick extends below grade, fill brick cavity solid to level of flashing and slope mortar slightly to outside under flashing.

- When flashing is to be laid on or against masonry, the surface of the masonry shall be smooth and free from projections which might puncture the flashing material.

- Where fresh masonry joins masonry that is partially set or totally set, the exposed surface of the set masonry shall be cleaned and lightly wetted so as to obtain the best possible bond with the new work.  All loose brick and mortar shall be removed.

- Expansion Joints:

  - Vertical:  Locate where indicated on drawings.  Lay units to form a vertical joint free of mortar and of same width as normal head joint UNO.

  - Horizontal:  Locate under shelf angles and other dissimilar materials abutted by brick.  Maintain a clear space at least 1/4-inch thick free of mortar. Inspect with trowel before installing backer rod and sealant.

  - Sealant:  Shall be in accordance with Section 07920.

3.02	FLASHINGS

Build in, as the work progresses all flashings which enter the masonry using the material and following the instructions of the appropriate section of the specifications.

Extend all flexible flashing 1” past face of wall and trim after tooling joints.

Where metal flashing or drip edge is shown, align drip with face of brick. Edge of flashing or drip edge shall be a simple hem rolled edge and not turned down.

3.03	OPENINGS AND HOLES

- Provide all openings and holes in masonry work.  Provide all chases and recesses in masonry work of all types as indicated on the drawings and as required for pipes, ducts, and other work of Mechanical and Electrical contractors.  Such work shall be accurately located by the contractor requiring the work, but masonry work shall not be constructed without giving other contractors due notices and opportunity to lay out or install such items as may be required for their work.

- Where required for installation of work of other contractors, leave openings as indicated on the drawing or as required to receive a later installation.

- After work of other contractors is in place, openings shall be neatly filled with masonry of the same type as in the adjoining surfaces.

3.04	SETTING AND BUILDING-IN

- Build-in materials occurring in any type of masonry construction that are furnished by other contractors.  All built-in work shall be accurately placed, secured, held in position, and located by the contractor requiring the work.

- Set and built -in items of miscellaneous iron such as loose lintels and anchors required to complete all parts not connected to building framing.

- Set all anchor bolts required for the attachment of work to masonry.

- Build-in recesses, flashings, receivers, slots, anchors, sleeves and other work shown on Drawings.

3.05	PROTECTION

- At the end of each day’s work, cover the tops of walls with canvas or other suitable material weighted down to keep water out of wall.

3.06	CLEANING BRICKWORK

- After pointing is done and wall is dry, clean face brick surface with dry brush.

- After 3 days clean with water and mild detergent or cleaners recommended by brick manufacturer.  Do not use muriatic acid.

  - Wet brick surfaces thoroughly before applying cleaning solution.

  - Apply cleaning solution with bucket and brush or LOW PRESSURE spray.

  - Remove all stains and mortar streaks using stiff fiber bristle brush.

  - Rinse THOROUGHLY with water.

  - Protect windows, landscaping, and surrounding masonry surfaces from cleaning solution and rinse water.

END OF SECTION